## Slide 1: Status of Glasgow module production
Richard Bates
The University of Glasgow
K.Smith, R. Bates, A. Cheplakov, V. O’Shea
W. Bell, J. Melone, F. Doherty, M. Horn
SCT Meeting –22nd September 2003

## Slide 2: Overview
Pre-qualification
5 qualification modules
S-curves
Wirebonding
Multi-module testing
Conclusions

## Slide 3: Pre-qualification
Glasgow pre-qualified start of July
  2 Modules:
    M-O-040_20220240100028 – 3 un-bonded channels
    M-O-044_20220240100032
      Problems with fan-in
      Glue on fan-in during construction
      Three groups of un-bondable channels ( => 191 defects!)
      Remove these => 19 defects, 5 un-bonded (12 bad to start with)

## Slide 4: 5 qualification modules
4 Finished all Glasgow steps and in spec!
One requires rework of VDC chip wire bond
  Output of VDC bond wire touching VDC chip
  Then final electrical tests to be performed
Glasgow steps
  Wirebonding
  Thermal cycling
  Long term test
  Electrical Characterisation

## Slide 5: Modules
20220240100035
20220240100038
20220240100041
20220240100043
20220240100044
All in spec bar high noise on #44
  100 extra electrons
  Work in progress on VDC bonding
S-curve problems has delayed qualification request!

## Slide 6: Summary of 20220240100035
IV – good – see plot
13 bad channels (started with 10 defects)
0 un-bonded
T=9oC
Gain = 55.4
Noise: link0=1432ele, link1=1428ele
No: module = 7.53x10-6, link0=6.97x10-6, link1=6.81x10-6
TW: link0 = 10.3ns, link1 =10.2ns

## Slide 7: Summary of 20220240100035
T=20oC
RH<10%
I@150V
  502nA
I@350V
  656nA

## Slide 8: TW of 20220240100035
TW: link0 = 10.3ns link1 =10.2ns

## Slide 9: Summary of 20220240100038
IV – good – see plot
8 bad channels (started with 0 defects)
7 un-bonded
T=11oC
Gain = 56.0
Noise: link0=1408ele, link1=1421ele
No: module = 5.4x10-5, link0=5.6x10-5, link1=5.5x10-5
TW: link0 = 10.1ns, link1 =10.4ns

## Slide 10: Summary of 20220240100038
T=20oC
RH<10%
I@150V
  266nA
I@350V
  420nA

## Slide 11: TW of 20220240100038
TW: link0 = 10.1ns link1 =10.4ns

## Slide 12: Summary of 20220240100041
IV – good – see plot
18 bad channels (started with 12 defects)
6 un-bonded
T=10oC
Gain = 54.7
Noise: link0=1478ele, link1=1499ele
No: module = 1.3910-5, link0=8.46x10-6, link1=1.12x10-5
TW: link0 = 10.4ns, link1 =10.9ns

## Slide 13: Summary of 20220240100041
T=20oC
RH<10%
I@150V
  430nA
I@350V
  594nA

## Slide 14: NO of 20220240100041

## Slide 15: TW of 20220240100041
TW: link0 = 10.4ns link1 =10.9ns

## Slide 16: LongTerm test of 20220240100041

## Slide 17: Summary of 20220240100043
IV – good – see plot
25 bad channels (started with 10 defects) (just in spec!)
11 un-bonded, 1 part-bonded
T=11oC
Gain = 54.4
Noise: link0=1503ele, link1=1506ele
No: module = 2.90x10-5, link0=3.35x10-5, link1=3.13x10-5
TW: link0 = 10.8ns, link1 =11.6ns

## Slide 18: Summary of 20220240100043
T=20oC
RH<10%
I@150V
  318nA
I@350V
  523nA

## Slide 19: TW of 20220240100043
TW: link0 = 10.8ns link1 =11.6ns

## Slide 20: LongTerm Test of 20220240100043

## Slide 21: Summary of 20220240100044
IV – good – see plot
1 bad channels (started with 1 defect)
0 un-bonded
T=8oC
Gain = 51.2
Noise: link0=1640ele, link1=1655ele
No: module = 7.53x10-6, link0=6.97x10-6, link1=6.81x10-6
TW: link0 = 10.0ns, link1 =10.3ns

## Slide 22: Summary of 20220240100044
T=20oC
RH<10%
I@150V
  215nA
I@350V
  338nA

## Slide 23: TW of 20220240100044
TW: link0 = 10.0ns link1 =10.3ns

## Slide 24: S-curves
Measurements made
  In Valencia test box
  Inside metal enclosure
  AERO r/o
  Shielded twisted pair power cables with KEK style chokes
  Shielded TP signal cables + ferrite chokes near patch card
Tried many grounding schemes
  Unable to remove discontinuity
Problem due to degradation of electrical contact between module and cooling block during cooling?
  To try spring washer

## Slide 25: Wirebonding Summary
Some lost bonds : average = 4.8 + 1 part-bonded
All chip to fan-in bonds
Lost bonds due to jig
  Only holds hybrid on edges – slight bounce
  Improved jig by holding module at mounting point
  No support on fan-in as this is of unknown height
Used for #44
  0 un-bonded

## Slide 26: Multi-module testing
All measurements to date done in single enclosure with capability for two modules
Second DAQ for multi-module testing present
All hardware present – waiting for final grounding scheme

## Slide 27: Conclusions
Not quite there yet!
Need to understand s-curve problem
Transfer grounding to multi-module set-up
Hope to make progress during this week on s-curves